PRODUCT DESCRIPTION

Oil UK Dexron VI is a premium quality, fully synthetic automatic transmission fluid for commercial and passenger car gearboxes meeting a very wide range of specifications. The automatic transmission is one of the most complicated mechanisms in modern automotive engineering and consequently requires complex fluids for efficient operation. Dexron VI is manufactured from premium synthetic base stocks and specially selected additives and friction modifiers to produce a lubricant with outstanding durability. It demonstrates excellent friction and wear protection, superior shear stability and offers extended fluid life even when under the most severe conditions.

- Long oil life

- Suitable for use as a power steering fluid

- Excellent Protection against wear

- Compatible with all elastomers and other sealing materials

- High temperature stability

- Provides ultimate component protection

APPLICATIONS

Dexron VI is recommended for step type automatic transmissions and power steering units in cars, vans, trucks, buses, agricultural and industrial machines where the following specifications are required:

TYPICAL PHYSICAL DATA

| Appearance | Clear, red liquid |
| --- | --- |
| Specific Gravity @ 15.6°C | 0.845 |
| Kinematic Viscosity @ 100°C (cSt) | 6.00 |
| Brookfield Viscosity @ -40°C (cP) | 12,030 |
| Flash Point PMCC (°C) | 190 |
| Pour Point °C | -53 |

PERFORMANCE SPECIFICATIONS

| General Motors | Dexron VI, Dexron IIIH, IIIG,IID, TASA |
| --- | --- |
| JASO | 1A |
| Allison | C4 |
| Caterpillar | TO-2 |
| Mercedes-Benz | 236.5 |
| Voith | 55.6335 (formerly G607) |
| Volvo | 97340 |
| ZF | TE-ML 09 |

In addition to the above performance specifications, OIL UK DEXRON VI is recommended for service fill in the following applications or where the following OEM genuine oils were originally required:

AISIN WARNER JWS 3309, JWS 3324, T IV, AW-1 FIAT (ALL VEHICLES), TYPO T IV SAAB T IV (JWS 3309)

AS 68 RC (T IV) HONDA / ACURA Z-1, PREMIUM SATURN T IV (JWS 3309)

AUDI 5 HP LT 71141 (ZF 5 HP 18FL / 19FL / 24A) HYUNDAI/ KIA SP II, SP III, SP IV & HYUNDAI SPH-IV SCION (ALL VEHICLES)

AUDI 5 HP LT 71141 (AUDI G-052-162-A1 / A2) NISSAN / INFINITY MATIC D, MATIC J, MATIC K, MATIC S SHELL M 115

AUDI 5 HP (ZF 5 HP 30) ISUZU BESCO ATF II, ATF III SUBARU ATF, ATF HP

AUDI G-055-025-A2 (JWS 3309) JAGUAR ATF 3403 M115, LT 71141, JLM 20238, SUZUKI ATF 3309

BMW ETL-7045, 7045E, JWS 3309 (T IV) TEXACO ETL-7045E

BMW LA2634, JWS 3324 (WS) TEXACO ETL-8072B

BMW 5 HP LT 71141 (ZF 5 HP 18FL / 19FL / 24A) MAZDA ATF M III

TOYOTA TYPE T-III, T-IV (JWS 3309)

BMW 5 HP (ZF 5 HP 30)

MERCEDES BENZ ZF HP20, 236.1, 236.5, 236.6, 236.7, 236.8, 236.9

TOYOTA WS (JWS 3324)

BMW ETL-8072B, MITSUBISHI DIAMOND SP II, SP III, SP IV, VOLVO T IV (JWS 3309)

BMW MINI JWS 3309 NAG 1

VW 5 HP LT 71141 (ZF 5 HP 18FL / 19FL / 24A)

CHRYSLER/DODGE MOPAR AS 68 RC (T IV) OPEL (All Vehicles)

VW 5 HP LT 71141 (VW G-052-162-A1 / A2)

DAEWOO LT 71141 PEUGEOT ZF 4 HP20 VW 5 HP (ZF 5 HP 30)

ESSO LT 71141 PORSCHE ATF 3403-M115, LT 71141, T IV (JWS 3309)

VW G-055-025-A2 (JWS 3309)

FORD WSS-M2C938-A