PRODUCT DESCRIPTION

OIL UK AUTOTRANS CVT is a high performance, fully synthetic transmission fluid designed to provide optimum performance in a wide range of continuously variable transmission (CVT) equipped passenger vehicles.

The specialised performance additive package incorporated into Autotrans CVT has demonstrated equal, and in many cases better, performance than most OEM supplied fluids in areas such as metal to metal wear protection of belt elements and pulleys.

APPLICATIONS

Autotrans CVT is recommended for a use in a wide range of passenger car vehicles fitted with continuously variable transmissions. In particular, Autotrans CVT can be used where any of the following specifications / OEM fluids is required. Autotrans CVT should NOT be used in conventional stepped automatic transmissions, DCT (Dual Clutch Transmissions), manual transmissions or Toyota e-CVT (THS, Toyota Hybrid System).

BENEFITS

- Exceptional shear stability

- Low temperature fluidity

- Low foaming

- Excellent oxidation resistance

- Anti-shudder durability

- Excellent wear protection

PERFORMANCE LEVEL SPECIFICATIONS

Audi / VW G 052 516, TL 52180, G 052 180 A1/A2/A6 Ford CFT30, WSS-M2C933-A, Mercon C, CFT23 Honda HMMF, HCF-2 Toyota / Lexus TC Nissan NS-1, NS-2 Mitsubishi CVTF-J1 Mazda CVTF 3320 Subaru i-CVTF, Lineartronic CVTF, K0425Y0710, CV-30, e-CVTF Mini Cooper EZL 799, EZL 799A, ZF CVT V1 Hyundai / Kia SP-CVT 1 Suzuki CVTF 3320, TC, NS-2, CVT Green 1 Dodge / Jeep NS-2 , CVTF+4, MOPAR CVT 4 GM /Saturn DEX-CVT Mercedes-Benz 236.20, CVT 28 Renault ELFMATIC BMW 8322 0 136 376, 8322 0 429 154 (EZL799, EZL 799A)

Autotrans CVT is also suitable for use out of warranty where the following low viscosity fluids were specified:

Nissan NS-3 GM / Saturn CVTF I-Green2 Mitsubishi CVTF-J4 Suzuki CVTF Green 2 Toyota / Lexus FE FE

TYPICAL PHYSICAL DATA

| Test | Units | Typical Properties |
| --- | --- | --- |
| Appearance |  | Red Fluid |
| Kinematic Viscosity @ 100°C | cSt | 7.2 |
| Kinematic Viscosity @ 40°C | cSt | 33.7 |
| Viscosity Index |  | 185 |
| Flash Point (Open) | °C | 200 |
| Pour Point | °C | -48 |
| Brookfield Viscosity @ -40°C | cP | 9020 |