PRODUCT DESCRIPTION

OIL UK GEARLUBE SY-PAO range consists of synthetic, high performance gear lubricants designed to operate in extreme conditions whilst maintaining optimum component and lubricant life. This synthetic range of lubricants is formulated with superior synthetic Polyalphaolefin base oils and a carefully balanced, state-of-the-art additive system which is designed to protect against scuffing and reduce fatigue related failures caused by issues such as micro-pitting.

APPLICATIONS

OIL UK GEARLUBE SY-PAO Gear Lubricants allow thermally stable operation at temperatures in excess of 200˚C. Typical applications include the lubrication of calendars, piston compressors and bevel, spiral bevel, helical, enclosed spur and worm gear units.

FEATURES AND BENEFITS

- Very high levels of wear protection

- Extended oil drain periods

- Excellent load carrying properties

- Outstanding oxidation stability and resistance to thermal breakdown

- Free from mineral oil, sulphur and chlorine

- Free from metal based additives including lead

- High load carrying properties

- Non-staining towards yellow metals

PERFORMANCE LEVEL SPECIFICATIONS

DIN 51517 Part 3, AGMA 9005-E02 (EP), US Steel 224, Flender Industrial Gear Rev. 9 (2005)

David Brown S1.53.101 (E)

TYPICAL PHYSICAL DATA

| Characteristic | ISO 32 | ISO 46 | ISO 68 | ISO 100 | ISO 150 | ISO 220 | ISO 320 | ISO 460 | ISO 680 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Specific Gravity @ 15°C | 0.848 | 0.850 | 0.851 | 0.853 | 0.854 | 0.855 | 0.856 | 0.856 | 0.857 |
| Kinematic Viscosity @ 40°C | 29.7 | 45.1 | 67.3 | 108.0 | 158.0 | 217.0 | 335.0 | 475.0 | 680.0 |
| Kinematic Viscosity @ 100°C | 5.7 | 7.8 | 10.7 | 15.0 | 21.0 | 26.0 | 37.0 | 48.0 | 63.0 |
| Viscosity Index | 136 | 143 | 148 | 145 | 156 | 152 | 158 | 160 | 162 |
| Flash Point °C | 238 | 245 | 255 | 265 | 265 | 265 | 265 | 265 | 265 |
| Pour Point °C | -45 | -45 | -43 | -42 | -42 | -40 | -40 | -36 | -24 |