OIL UK AQUA-GUARD SLIDEWAY OILS UNIQUE RANGE OF SLIDEWAY LUBRICANTS THAT PREVENT TRAMP OIL EMULSIFICATION

DESCRIPTION

OIL UK Aqua-Guard Slideway Oils are a super advanced range of specially designed mineral oil based Slideway lubricants which overcome many of the problems associated with leakage into and contamination of and by soluble cutting fluids. With the ultra-efficient Aquatron additive package demulsification performance is truly exceptional. It will reject coolant contamination and will separate faster than any other Slideway fluid from coolant

making oil removal faster and more effective, keeping the coolant cleaner and therefore in superior condition. The oil can be removed more efficiently from the sump. This leads to better sump-life, system cleanliness, and coolant concentration control.

AQUA-GUARD HELPS TO MINIMISE TRAMP OIL CONTAMINATION BY PREVENTING EMULSIFICATION

AND KEEPING THE OIL SEPARATE FROM THE COOLANT, ENABLING IT TO BE SKIMMED OFF.

| TYPICAL PHYSICAL DATA |
| --- |
| PROPERTY | UNIT | TEST METHOD | Aqua-Guard 32 | Aqua-Guard 68 | Aqua-Guard 220 |
| Appearance |  |  | Amber | Amber | Amber |
| Specific Gravity @ 15.6°C | g/ml | ASTM D4052 | 0.84 | 0.85 | 0.88 |
| Kinematic Viscosity @ 40°C | cSt | ASTM D445 | 32 | 68 | 220 |
| Viscosity Index |  | ASTM D2270 | 100 | 100 | 100 |
| Demulsification |  | ASTM D 1401 | 40-40-0 (5) | 40-40-0 (5) | 40-40-0 (5) |
| Demulsification (In-house 5 parts coolant 75 parts oil) |  | 75-5-0 (5) | 75-5-0 (5) | 75-5-0 (5) |
| Demulsification (In-house 75 parts coolant 5 parts oil) |  | 5-75-0 (5) coolant unchanged in appearance | 5-75-0 (5) coolant unchanged in appearance | 5-75-0 (5) coolant unchanged in appearance |
| IP135 B (mod 5%coolant) | IP135 B | Pass | Pass | Pass |
| IP287 (5% Slideway oil in coolant) | IP287 | Unchanged | Unchanged | Unchanged |