OIL UK MACHINE-LUB GP HIGH QUALITY INDUSTRIAL MACHINE LUBRICANTS

DESCRIPTION

OIL UK MACHINE-LUB GP is a range of highly refined, non-additive general-purpose lubricants. This high quality range of machine oils are manufactured using superior, highly refined base oils. They exhibit extremely good oxidation stability and rust prevention, and resist the formation of harmful gums and lacquers.

OIL UK MACHINE-LUB GP lower viscosity grades are designed for use in machine circulatory systems. The higher viscosity grades are suitable for gear systems when a non-EP, additive-free grade is required.

| TYPICAL PHYSICAL DATA | VISCOSITY GRADE & TYPICAL PROPERTIES |
| --- | --- |
| PROPERTY | UNIT | 3 | 5 | 10 | 15 | 22 | 32 | 46 |
| Specific Gravity @ 15.5°C | g/ml | 0.826 | 0.827 | 0.850 | 0.860 | 0.868 | 0.872 | 0.878 |
| Kinematic Viscosity @ 100°C | cSt |  |  | 2.59 | 3.41 | 4.31 | 5.41 | 6.79 |
| Kinematic Viscosity @ 40°C | cSt | 4.04 | 5.06 | 9.84 | 15.17 | 21.97 | 32.01 | 46.02 |
| Viscosity Index |  |  |  | 90 | 95 | 101 | 101 | 102 |
| Flash Point (Open) | °C | 145 | 145 | 162 | 183 | 195 | 215 | 220 |
| Pour Point | °C | -25 | -20 | -18 | -14 | -12 | -12 | -12 |
|  |  | 68 | 100 | 150 | 220 | 320 | 460 | 680 |
| Specific Gravity @ 15.5°C | g/ml | 0.880 | 0.888 | 0.890 | 0.894 | 0.896 | 0.901 | 0.917 |
| Kinematic Viscosity @ 100°C | cSt | 8.79 | 11.40 | 15.11 | 19.40 | 25.02 | 31.28 | 34.68 |
| Kinematic Viscosity @ 40°C | cSt | 68.05 | 100.03 | 150.09 | 219.88 | 319.98 | 462.11 | 644.40 |
| Viscosity Index |  | 102 | 100 | 101 | 100 | 100 | 98 | 85 |
| Flash Point (Open) | °C | 224 | 228 | 231 | 233 | 234 | 245 | 268 |
| Pour Point | °C | -12 | -12 | -11 | -10 | -10 | -9 | -9 |