OIL UK MACHINE-LUB UNIVERSAL HIGH QUALITY MULTI-FUNCTIONAL INDUSTRIAL LUBRICANTS

DESCRIPTION

OIL UK MACHINE-LUB UNIVERSAL is a range of premium quality, ashless, multi-functional oils designed to satisfy the needs of machine tools and general factory equipment. These grades exhibit outstanding demulsifying properties making them the first choice for use as slideway oils with water based metalworking coolants. When in contact with the coolant, very rapid separation of the lubricant allows for quick and easy removal.

Machin-Lub Universal grades possess excellent anti-wear, extreme pressure, lubricity and rust protection properties along with a high degree of oxidation resistance. This makes them the ideal choice for gear and hydraulic applications allowing for product rationalisation and stock inventory reduction.

APPLICATIONS

Recommended for a wide variety of machine lubrication requirements. In particular, Machine-Lub Universal grades are highly effective machine tool slideway lubricants and demonstrate excellent performance in hydraulic, industrial gear and bearing applications.

PERFORMANCE SPECIFICATIONS

DIN 51524 - 2 HLP, DIN 51517 - 3 CLP, Cincinnati Lamb P-47 (ISO 68 grade)

| TYPICAL PHYSICAL DATA | VISCOSITY GRADE & TYPICAL PROPERTIES |  |
| --- | --- | --- |
| PROPERTY | UNIT | 32 | 46 | 68 | 100 | 150 | 220 | 320 | 460 |
| Specific Gravity @ 15.6°C | g/ml | 0.872 | 0.875 | 0.880 | 0.883 | 0.890 | 0.895 | 0.899 | 0.903 |
| Kinematic Viscosity @ 100°C | cSt | 5.33 | 6.70 | 8.60 | 11.20 | 14.70 | 19.00 | 24.20 | 30.50 |
| Kinematic Viscosity @ 40°C | cSt | 32 | 46 | 68 | 100 | 150 | 220 | 320 | 460 |
| Viscosity Index |  | 98 | 97 | 97 | 97 | 96 | 96 | 96 | 96 |
| Flash Point (Open) | °C | 215 | 224 | 234 | 246 | 255 | 260 | 275 | 298 |
| Pour Point | °C |  |  |  |  |  |  |  |  |