PRODUCT DESCRIPTION

OIL UK VALIANT HT are premium quality, low carbon forming, ash free compressor oils.

Lubricants for compressors vary dependent upon the type of compressor (e.g. reciprocating, rotary, screw) and also the gas being compressed (e.g. air, nitrogen and refrigerants etc.).  With these features firmly in mind the Valiant HT range has been designed for a large variety of manufacturers’ specifications and requirements.

The Valiant HT range of compressor oils are manufactured using carefully selected mineral oils. Inhibitors are added to control oxidation, a problem encountered in the high temperature areas of the discharge zones and anti-wear additives protect all the mechanical parts in the compressor.

Compressor HT oils are designed for a minimum 2000 hour service life under normal operating conditions.   Performance Specification:  DIN 51506 VD-L

APPLICATIONS

OIL UK VALIANT HT 22, 32 and 46 are recommended for the lubrication of screw type compressors. Valiant HT 68 and HT 100 are recommended for the lubrication of reciprocating (piston) type compressors. Both Valiant HT 68 and HT 100 can be used in sliding vane applications where oils of these viscosities are required. Valiant HT 150 is suitable for the lubrication of sliding vane compressors.

It is vitally important when selecting the required lubricant that the equipment manufacturer’s recommendation is adhered to. Always comply with the manufacturer’s drain periods.

FEATURES AND BENEFITS

- Excellent oxidation stability

- Low evaporation and carry over

- Excellent moisture separation

TYPICAL PHYSICAL DATA

|  |  | VALIANT HT VISCOSITY GRADE & TYPICAL PROPERTIES |
| --- | --- | --- |
|  | Units | 22 | 32 | 46 | 68 | 100 | 150 |
| Appearance |  | Straw | Straw | Amber | Amber | Amber | Amber |
| Specific Gravity @ 15.6°C |  | 0.861 | 0.874 | 0.877 | 0.880 | 0.888 | 0.890 |
| Kinematic Viscosity @ 40°C | cSt | 22 | 32 | 46 | 68 | 100 | 150 |
| Pour Point °C |  | -18 | -12 | -12 | -11 | -11 | -11 |
| Flash Point °C |  | 195 | 215 | 219 | 224 | 227 | 230 |
| Viscosity Index |  | 100 | 102 | 102 | 102 | 100 | 101 |