PRODUCT DESCRIPTION

OIL UK VALIANT PAO is a range of fully synthetic compressor oils blended from ultra-pure synthetic hydrocarbons, synthetic ester and fortified with sophisticated additives to ensure long term protection and reliability. Oil drain intervals of up to 8000 hours can be achieved. Benefits provided include reduced maintenance downtime, extremely low evaporative loss, high resistance to deposit formation and oxidation and superb load carrying and anti-wear characteristics.

PERFORMANCE SPECIFICATIONS

DIN 51506 VD-L, DIN 51524 PART 3, AFNOR NFE 48-603 (HM), SPERRY VICKERS I-286-S, CINCINNATI MILACRON P-69

FEATURES AND BENEFITS

Recommended for single & multi-stage compressors • They offer extended oil life thereby reducing servicing and downtime • Good seal and paint compatibility • Extremely low evaporative loss - less oil thickening • Excellent demulsibility • High resistance to oxidation & deposit formation • Superb load carrying & anti-wear characteristics • Outstanding viscosity / temperature characteristics

APPLICATIONS GUIDE

| Product | Valiant PAO 32 | Valiant PAO 46 | Valiant PAO 68 | Valiant PAO 100 | Valiant PAO 150 |
| --- | --- | --- | --- | --- | --- |
| Compressor Type | Screw | Vane | Piston | Reciprocating | Hydrovane |

PERFORMANCE SPECIFICATIONS

DIN 51506 VDL DIN 51524 part 3 (HVLP), Afnor NF E 48-603 (HM), Sperry Vickers I-286-S,

Cincinnati Milacron P-68 (ISO 32), P-69 (ISO 68), P-70 (ISO 46)

TYPICAL PHYSICAL DATA

|  |  | PAO 32 | PAO 46 | PAO 68 | PAO 100 | PAO 150 |
| --- | --- | --- | --- | --- | --- | --- |
| Specific Gravity @ 15.6°C |  | 0.876 |  |  |  |  |
| Kinematic Viscosity @ 40°C | cSt | 33.30 | 47.40 | 68.20 | 98.10 | 148.30 |
| Kinematic Viscosity @ 100°C | cSt | 6.30 | 7.90 | 10.50 | 13.90 | 16.40 |
| Pour Point °C |  | -40 | -40 | -40 | -40 | -40 |
| Flash Point °C |  | >250 | >250 | >250 | >250 | >250 |