PRODUCT DESCRIPTION

OIL UK VALIANT FRC is a range mineral oil based refrigeration compressor oil for use in a variety of industrial refrigeration compressors. These products are manufactured using carefully selected base oils which possess inherently low temperature capabilities which reduces the formation of ice crystals if water is present in the lubricant and remains fluid even at the lowest temperatures encountered in the operating cycle. Valiant FRC oils are compatible with various refrigerants including freon (R22), ammonia and carbon dioxide.

FEATURES AND BENEFITS

- Excellent low temperature performance

- Improved evaporator efficiency

High levels of system cleanliness

APPLICATIONS GUIDE

Valiant FRC grades are suitable for domestic and industrial refrigeration compressors with any of the following refrigerants: Ammonia (R717), Hydrocarbon (e.g. R600a), Halogenated hydrocarbon (R12, R22)

TYPICAL PHYSICAL DATA

|  |  | FRC 32 | FRC 46 | FRC 68 |
| --- | --- | --- | --- | --- |
| Specific Gravity @ 15.6°C |  | 0.873 | 0.878 | 0.880 |
| Kinematic Viscosity @ 40°C | cSt | 32 | 46 | 68 |
| Kinematic Viscosity @ 100°C | cSt | 5.36 | 6.75 | 8.75 |
| Pour Point °C |  | -35 | -33 | -32 |
| Flash Point °C |  | 215 | 220 | 224 |