VERY HIGH PERFORMANCE HEAVY DUTY SOLUBLE METALWORKING FLUID DESIGNED FOR MULTIPLE APPLICATIONS

PRODUCT DESCRIPTION

SOLCUT 5000 has been formulated to cross all performance boundaries. The formulation is based on a unique additive combination working in perfectly balanced synergy to enable neat oil applications such as broaching and gear cutting to be considered for a switch to water soluble technology. This super high performance product is also inherently low foaming and is a perfect choice for use in both hard and soft water conditions. SOLCUT 5000 is a superb choice of fluid for every difficult application.

APPLICATIONS

### SOLCUT 5000 offers excellent cutting performance and can be used in all types of arduous manufacturing applications. The performance additives incorporated into the fluid provide outstanding surface finish on all types of aluminium and associated alloys as well in addition to tougher materials such as high tensile steels. The unique formulation is suitable for both hard and soft waters and prevents scum and soap formation associated with more reactive materials. SOLCUT 5000 has been proven to have outstanding tool life performance when used in the machining of titanium as well as demonstrating superb properties when used in the machining of high tensile steels.

FEATURES AND BENEFITS

- Excellent high sheer performance and outstanding boundary and hydrodynamic lubrication

- Loaded with lubricity components for enhanced tool life and excellent surface finish

- Suitable for both moderate and highly arduous applications

- Low foaming tendency in high pressure systems and suitable for both hard and soft water qualities

- Multi-metal compatible. Suitable for both ferrous and non-ferrous materials

- Provides long, low odour coolant life and excellent machine tool cleanliness

- Excellent cost saving potential through enhanced tool life

- Extra high levels of corrosion protection

| MATERIAL SUITABILITY AND RECOMMENDED CONCENTRATIONS |
| --- |
| Material Type | Performance Rating | Machining Application | Recommended Concentration |
| Titanium | xxxxx | Broaching | 8-10% |
| Aluminium | xxxx | Tapping | 6-10% |
| Aerospace Aluminium Alloys | xxxx | Milling | 5-7% |
| High Alloy / Stainless Steels | xxxxx | Turning | 5-7% |
| Copper / Brass | xxx | Reaming | 8-10% |
| Cast Iron | xx | Sawing | 5-8% |
|  |  | Drilling | 7-10% |

| TYPICAL PHYSICAL DATA |
| --- |
| Appearance of Concentrate: | Amber liquid |
| Odour: | Sweet |
| Emulsion Appearance: | Milky white |
| Specific Gravity: | 0.985 |
| pH @ 5%: | 9.2 |
| IP287 Breakpoint, %: | 2.5 |
| IP125 Breakpoint, %: | 2.0 |
| Stack Corrosion Test | 2.0 |
| De-foam in 50p.p.m. water: | Nil after 10 seconds |
| Reichert Performance @ 10%: | Noise Reduction 5.0m Load Capacity 3.59Kg/mm2 |
| Refractometer Correction Factor: | 1.1 |
| Aluminium Stain Test | No Stain |

Product Mixing:

OIL-UK advise the use of automated mixing systems. If mixing manually, always add the concentrate to the water with maximum agitation, if water is added to the concentrate, the emulsions may prove unstable. Avoid mixing with very cold concentrate or water. Check emulsion strength using a calibrated refractometer. Details of where to purchase equipment and how to use it are available from the OIL-UK Technical Department.

Product Management:

The working concentration should be carefully controlled and monitored on a daily basis as higher and lower working concentrations have health and safety implications. Machines should be cleaned out regularly. Fluid and particulate contaminants should be kept to a minimum. This is important especially in terms of bacterial control and is in line with the latest advice from government and professional sources. Detailed reference sources are quoted in the MSDS

Storage:

- Store in a cool, well ventilated area

- Store inside, ideally between 10°C and 30°C

- Store away from direct heat and frost

- Shelf life 12 months from the date of manufacture

- Avoid water collecting on the barrel top