### HIGH PERFORMANCE WATER-MIX METALWORKING FLUID DESIGNED FOR ULTRA-LONG SUMP LIFE UNDER ARDUOUS OPERATING CONDITIONS

PRODUCT DESCRIPTION

SOLCUT ULTRALIFE is a low mineral oil content high performance semi-synthetic soluble metalworking fluid that produces an ultra-stable translucent emulsion. This product has been designed to provide the maximum possible sump life, even in highly arduous operating conditions. SOLCUT ULTRALIFE is particularly low foaming in high pressure systems soft water conditions, and the emulsion remains clean even in hard water. This formulation has been developed to cross all performance boundaries, and is based upon a unique performance enhancing additive combination working in perfect balanced synergy to enable use in extremely arduous applications. SOLCUT ULTRALIFE is an excellent choice for heavy duty applications where ultra-long sump life is a key consideration.

APPLICATIONS

SOLCUT ULTRALIFE offers excellent cutting performance and is suitable for machining a wide variety of materials including high tensile and stainless steels, aluminium alloys, cast iron high density plastics and other difficult to machine materials.

FEATURES AND BENEFITS

- Ultra-long sump life

- Excellent machining performance

- Outstanding tool life performance

- Multi-metal compatible

- Ultra-low foaming tendency

- High levels of boundary & hydro-dynamic lubrication

- Suitable for high pressure systems using hard or soft water qualities

- Excellent surface finish

MATERIALS SUITABILITY AND RECOMMENDED CONCENTRATIONS

| Material Type | Performance Rating | Machining Applications | Recommended Concentration |
| --- | --- | --- | --- |
| Aluminium | XXXX | Tapping | 6-10% |
| Aerospace Aluminium Alloys | XXXX | Milling | 5-7% |
| High Alloy/Stainless Steels | XXXXX | Turning | 5-7% |
| Copper/Brass | XXX | Reaming | 8-10% |
| Cast Iron | XXXX | Sawing | 5-8% |
| Plastics | XXXXX | Drilling | 7-10% |

TYPICAL PHYSICAL CHACTERISTICS

| Characteristic | Typical Test Result |
| --- | --- |
| Appearance | Amber Fluid |
| Emulsion Type | Translucent |
| Foaming Tendency | Low |
| Specific Gravity | 1.03 |
| pH @ 5% Dilution | 9.5 |
| IP 287 Corrosion Break Point % Vol | 2.0 |
| IP 125 Corrosion Break Point % Vol | 2.0 |
| Defoam ml (3% in 50ppm water) | Nil @ 7 Seconds |
| Refractometer Factor | 1.4 |
| Reichert Lubricity Characteristics (10% dilution). Noise Reduction: Load Bearing Capacity (5% dilution): | 11.0 metres 3.17 |
| Aluminium Stain Test | No Stain |

Product Mixing

OIL-UK advise the use of automated mixing systems. If mixing manually, always add the concentrate to the water with maximum agitation, if water is added to the concentrate, the emulsions may prove unstable. Avoid mixing with very cold concentrate or water. Check emulsion strength using a calibrated refractometer. Details of where to purchase equipment and how to use it are available from the OIL-UK Technical Department.

Product Management

The working concentration should be carefully controlled and monitored on a daily basis as higher and lower working concentrations have health and safety implications. Machines should be cleaned out regularly. Fluid and particulate contaminants should be kept to a minimum. This is important especially in terms of bacterial control and is in line with the latest advice from government

Storage

- Store in a cool, well ventilated area

- Store inside, ideally between 10°C and 30°C

- Store away from direct heat and frost

- Shelf life 12 months from the date of manufacture

Avoid water collecting on the barrel top