### ULTRA-LONG LIFE SOLUBLE METALWORKING FLUID DESIGNED FOR ARDUOUS CONDITIONS USING SOFT WATER UNDER HIGH PRESSURE

PRODUCT DESCRIPTION

OIL UK SOLCUT ULTRALIFE X is a high performance, multifunctional semi synthetic metal process fluid which produces a translucent micro emulsion when diluted in water.  This product has been designed for use in a variety of water qualities, but is particularly effective in high pressure systems using soft water, where it provides excellent foam control and outstanding machining performance

SOLCUT ULTRALIFE X is based upon synthetic and natural esters with surface active agents to provide excellent machining performance across a wide range of arduous machining applications.

APPLICATIONS

OIL UK SOLCUT ULTRALIFE X is the perfect fluid for use in applications such as automotive car parts manufacturing where maximum tool life is expected and where ongoing cost savings are demanded. The performance enhancing additive system provide outstanding surface finish on all types of materials from aluminium alloys to high tensile and stainless steels. .

FEATURES AND BENEFITS

- Ultra-long sump life

- Excellent arduous machining performance

- Reduces Tooling Costs

- Low product consumption

- Ultra-low foaming tendency

- High levels of boundary & hydra-dynamic lubrication

- Loaded with performance additives

MATERIAL SUITABILITY AND RECOMMENDED CONCENTRATIONS

| Material Type | Performance Rating | Machining Applications | Recommended Concentration |
| --- | --- | --- | --- |
| Titanium | XXXX | Tapping | 6-10% |
| Aluminium | XXXX | Milling | 5-7% |
| High Alloy/Stainless Steels | XXXXX | Turning | 5-7% |
| Copper/Brass | XXX | Reaming | 8-10% |
| Cast Iron | XXXX | Sawing | 5-8% |
|  |  | Drilling | 7-10% |

TYPICAL PHYSICAL PROPERTIES

| Property | Typical Test Result |
| --- | --- |
| Appearance - Concentrate | Amber Fluid |
| Emulsion Type | Translucent |
| Foaming Tendency | Low |
| Specific Gravity | 1.04 |
| pH @ 5% | 9.4 |
| IP 287 Corrosion Test % | 2.0 |
| IP 125 Corrosion Test % | 2.0 |
| Defoam ml (3% in 50ppm water) | Nil @ 7 Seconds |
| Refractometer Factor | 1.4 |
| Reichert Lubricity Characteristics (10% dilution): Noise Reduction: Load Bearing Capacity (5% dilution) | 7.0 metres 3.67 |

Storage

- Store in a cool, well ventilated area

- Store inside, ideally between 10°C and 30°C

- Store away from direct heat and frost

- Shelf life 12 months from the date of manufacture

Avoid water collecting on the barrel top

Product Mixing

Oil UK advises the use of automated mixing systems. If mixing manually, always add the concentrate to the water with maximum agitation, if water is added to the concentrate, the emulsions may prove unstable. Avoid mixing with very cold concentrate or water. Check emulsion strength using a calibrated refractometer. Details of where to purchase equipment and how to use it are available from the Oil UK Technical Department.

Product Management

The working concentration should be carefully controlled and monitored on a daily basis as higher and lower working concentrations have health and safety implications. Machines should be cleaned out regularly. Fluid and particulate contaminants should be kept to a minimum. This is important especially in terms of bacterial control and is in line with the latest advice from government and professional sources. Detailed reference sources are quoted in the MSDS.