HIGH PERFORMANCE CHLORINE FREE SYNTHETIC SOLUBLE GRINDING FLUID FOR HIGH CARBIDE ALLOYS AND TUNGESTEN CARBIDES

PRODUCT DESCRIPTION

OIL-UK SOL-GRIND TC is an ultra-modern synthetic water-mix grinding fluid which minimises the uptake of cobalt alloys. This product provides excellent performance on tungsten carbide and high cobalt alloys, and displays exceptional resistance to cobalt leaching. It is also suitable for most ferrous and non-ferrous metals.

OIL-UK SOL-GRIND TC provides enhanced operator safety, prevents hazardous cobalt leaching, and is free from controversial components such as secondary amines, chlorine EP, Sulphur EP, Triazine biocides, sodium nitrite, silicone oil defoamers, phenolic couplers, nonyl phenol and NP ethoxylates, colouring dyes. This product exhibits excellent levels of anti-corrosion protection and cleanliness whilst demonstrating good swarf settlement.

OIL-UK SOL-GRIND TC produces a clear water-white emulsion to provide excellent work-piece visibility. The excellent anti-corrosion properties of this product give protection to machine tool surfaces and finished components. Minimal sticky deposits and residues can be expected from this high quality synthetic formulation.

OIL-UK SOL-GRIND TC is low foaming and suitable for a wide variety of water qualities from soft to hard (up to 500ppm Calcium Carbonate)

FEATURES AND BENEFITS

- Ultra-High Performance

- Long Sump Life

- Ultra-low cobalt leaching potential

- Improved Wheel Life

- Highly Stable Solution

- Low Irritant

- Operator Friendly

- Excellent Corrosion Protection

- Ultra-Low Foam

- No Sticky Deposits

MATERIALS SUITABILITY AND RECOMMENDED CONCENTRATIONS

| Material Type | Performance Rating | Machining Applications | Recommended Concentration |
| --- | --- | --- | --- |
| *Tungsten Carbide | XXXXX | Grinding | *5% Plus |
| Aluminium | XXX | Grinding | 5% Plus |
| Aerospace Aluminium Alloys | XX | Grinding | 5% Plus |
| High Alloy/Stainless Steels | XXX | Grinding | 5% Plus |
| Copper/Brass | XX | Grinding | 5% Plus |
| Cast Iron | XXXXX | Grinding | 5% Plus |
| A concentration of 5% minimum is required to avoid potential cobalt leaching when grinding Tungsten Carbide |

TYPICAL PHYSICAL PROPERTIES

| Characteristic | Typical Test Value |
| --- | --- |
| Appearance - Concentrate | Yellow / Amber Fluid |
| Specific Gravity - Concentrate | 1.12 |
| Foaming Tendency | Low |
| Appearance - Emulsion | Transparent |
| IP287 Corrosion Break Point % Vol | 3.0% |
| IP125 Corrosion Break Point % Vol | 3.0% |
| Refractometer factor | 1.2 |
| pH @ 5% Emulsion | 9.1 |

Product Mixing:

OIL-UK advise the use of automated mixing systems. If mixing manually, always add the concentrate to the water with maximum agitation, if water is added to the concentrate, the emulsions may prove unstable. Avoid mixing with very cold concentrate or water. Check emulsion strength using a calibrated refractometer. Details of where to purchase equipment and how to use it are available from the OIL-UK Technical Department.

Product Management:

The working concentration should be carefully controlled and monitored on a daily basis as higher and lower working concentrations have health and safety implications. Machines should be cleaned out regularly. Fluid and particulate contaminants should be kept to a minimum. This is important especially in terms of bacterial control and is in line with the latest advice from government and professional sources. Detailed reference sources are quoted in the MSDS.

Storage:

- Store in a cool, well ventilated area

- Store inside, ideally between 10°C and 30°C

- Store away from direct heat and frost

- Shelf life 12 months from the date of manufacture

- Avoid water collecting on the barrel top