OIL UK EDM CRYSTAL HIGH PERFORMANCE SYNTHETIC EDM FLUID

DESCRIPTION

OIL UK EDM CRYSTAL has been designed for use in both high and low amperage spark erosion processes. Its unique blend of ultra-pure hydrocarbons with the latest synthetic technology provides a crystal clear fluid with high oxidation stability and extremely low viscosity. The result is stability under high amperage as well as fast flushing in tight tolerance finishing work. OIL UK EDM CRYSTAL possesses low viscosity. This combined with the low specific gravity, means faster more efficient flushing and filtration. The result is increased metal removal rates, by as much as 30%. Filtration is improved due to less carbon and residue formation. The filter lasts longer and particulates are prevented from returning to the electrode work-piece interface. Safety – Additionally, benefits of Gulfcut EDM Crystal are in its safety and operator friendliness. The fluid is odourless and contains no solvent-based hydrocarbons. This helps eliminate skin irritation associated with solvents and reduces oil mist and solvent vapour exposure

| PERFORMANCE BENEFITS |
| --- |
| Enhanced Health & Safety | Good surface finish |
| Good detergency. | Good flushing |
| Cost effective | Very economical in-use |
| Synthetic | Superior performance |
| Highly treated | Long service life. |

TYPICAL PHYSICAL PROPERTIES

| Appearance | Clear fluid |
| --- | --- |
| Specific Gravity | ~0.85 @ 20oC |
| Foaming Tendency | Low |
| Viscosity at 40oC | 3 cSt |
| Flash Point °C | 130 |
| Anti-oxidation | Good |
| Chlorine (elemental) | Nil |
| Sulphur (active) | Nil |