OIL UK HYLOAD HLP PREMIUM ANTI-WEAR HYDRAULIC OILS RANGE

DESCRIPTION

The OIL UK HYLOAD HLP range of hydraulic fluids are high performance anti-wear grades designed for systems working under severe conditions in a large range of applications. These products are manufactured from highly refined base oils which possess excellent oxidation resistance and thermal stability. They are fortified with carefully selected additives to further improve performance characteristics, including anti-corrosion, and rapid demulsibility to protect the system should water be present, anti-wear to enhance equipment life in high pressure, high output pumps, anti-oxidants for long service life and special antifoam and air release properties.

APPLICATION

OIL UK HYLOAD HLP hydraulic oils are suitable for a wide variety of applications. These include high performance industrial hydraulic systems running under severe conditions, agricultural and plant equipment, mobile units such as jacks, lightly loaded gears and many others.

FEATURES AND BENEFITS

- Incorporates inhibitors for protection against all forms of corrosion

- Excellent anti-foaming and air release properties

- Good demulsification characteristics, ensuring rapid water separation

- Superb anti-wear performance, ensuring maximum component life

- Excellent oxidation resistance and thermal stability, providing enhanced service life

- Suitable for all hose materials used with mineral oil based hydraulic oils

PERFORMANCE SPECIFICATIONS

DIN 51524 Part 2, category HLP ISO 6743/4, category HM

Denison HF-2 TP-02100 Filterability Test

Sperry Vickers M-2950-S I-286-S Afnor  NF E 48-600 Thyssen  TH N-256132 US Steel  127 SEB 181.222 VDMA 24318

HYLOAD HLP HYDRAULIC OIL RANGE: TYPICAL PHYSICAL DATA

| HYLOAD HLP ISO VISCOSITY GRADE: | 3 | 5 | 10 | 15 | 22 | 32 | 37 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Specific Gravity @ 15.6°C | 0.822 | 0.827 | 0.850 | 0.860 | 0.865 | 0.873 | 0.875 |
| Kinematic Viscosity @ 40°C (cSt) | 3.0 | 5.0 | 10.0 | 15.0 | 22.0 | 32.0 | 37.0 |
| Kinematic Viscosity @ 100°C (cSt) | - | - | 2.62 | 3.38 | 4.29 | 5.36 | 5.87 |
| Viscosity Index | - | - | 91 | 95 | 100 | 100 | 100 |
| Flash Point °C | - | - | 162 | 183 | 195 | 215 | 217 |
| Pour Point °C | - | - | - | - | -33 | -33 | -33 |

| HYLOAD HLP ISO VISCOSITY GRADE: | 46 | 68 | 100 | 150 | 220 | 320 | 460 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Specific Gravity @ 15.6°C | 0.878 | 0.880 | 0.889 | 0.890 | 0.893 | 0.895 | 0.901 |
| Kinematic Viscosity @ 40°C (cSt) | 46.0 | 68.0 | 100.0 | 150.0 | 220.0 | 320.0 | 460.0 |
| Kinematic Viscosity @ 100°C (cSt) | 6.75 | 8.75 | 2.62 | 3.38 | 4.29 | 5.36 | 5.87 |
| Viscosity Index | 100 | 100 | 91 | 95 | 100 | 100 | 100 |
| Flash Point °C | 220 | 224 | 162 | 183 | 195 | 215 | 217 |
| Pour Point °C | -32 | -31 | -27 | -25 | -23 | -21 | -20 |