OIL UK HYLOAD HVLP PREMIUM HIGH VISCOSITY INDEX MULTIGRADE HYDRAULIC OILS RANGE

DESCRIPTION

The OIL UK HYLOAD HVLP grades are a range of specialist premium quality, very high viscosity index multigrade hydraulic fluids. The economical operation of a hydraulic system is dependent on the correct hydraulic oil being used. This range of hydraulic fluids is manufactured from highly refined base oils which have good oxidation resistance, lowering the possibility of gums and lacquers. They are blended using carefully selected additives and special viscosity index improvers which offer superior viscosity/temperature characteristics. They can be used where extremes of ambient temperatures are encountered

APPLICATION

OIL UK HYLOAD HVLP range of hydraulic oils is suitable for a wide range of industrial applications including those where low temperatures are encountered (frozen food stores etc.), as well agricultural and construction sectors.

FEATURES AND BENEFITS

- Excellent cold weather & high temperature performance

- Incorporates inhibitors for protection against all forms of corrosion

- Good anti-foaming and air release properties

- Good demulsification characteristics

- Excellent anti-wear performance

- High oxidation resistance and thermal stability

- Suitable for all hose materials used with mineral oil based hydraulic oils

PERFORMANCE SPECIFICATIONS

DIN 51524 Part 3, category HVLP 51517 Part 2, ISO 6743/4 category HV, Sperry Vickers S I-286-S

OIL UK HYLOAD HVLP PREMIUM HIGH VISCOSITY INDEX MULTIGRADE HYDRAULIC OILS RANGE

TYPICAL PHYSICAL DATA

| HYLOAD HVLP ISO VISCOSITY GRADE: | 15 | 22 | 32 | 46 | 68 | 100 |
| --- | --- | --- | --- | --- | --- | --- |
| Specific Gravity @ 15.6°C | 0.848 | 0.850 | 0.870 | 0.882 | 0.870 | 0.882 |
| Kinematic Viscosity @ 40°C (cSt) | 15.0 | 22.0 | 32.0 | 46.0 | 68.0 | 100.0 |
| Kinematic Viscosity @ 100°C (cSt) | 3.90 | 5.00 | 6.50 | 8.40 | 10.90 | 15.10 |
| Viscosity Index | 154 | 155 | 155 | 156 | 157 | 158 |
| Flash Point °C | 150 | 185 | 205 | 212 | 218 | 225 |
| Pour Point °C | -38 | -36 | -34 | -33 | -33 | -32 |