DESCRIPTION

The OIL UK HYLOAD ZF grades are a range of premium quality, zinc and ash free hydraulic fluids. The economical operation of a hydraulic system is dependent on the correct hydraulic oil being used. Many modern machines use hydraulic oils for the transmission of power from one component to another.

The HYLOAD ZF range of hydraulic fluids are manufactured from highly refined base oils, which have good oxidation resistance lowering the possibility of gums and lacquers. They are blended using the latest in additive technology. The ash free additive pack used reduces the possibility of sludge and ensures rapid water separation.

APPLICATION

OIL UK HYLOAD ZF range of hydraulic oils is suitable for a wide variety of applications. They are recommended for rotary, vane, axial piston, gear pumps and bearings in many types of circulating systems. They are ideal for machine tool applications were contact with the metalworking fluid can occur.

FEATURES AND BENEFITS

- Compatible with all component metals, including silver

- Incorporates inhibitors for protection against all forms of corrosion

- Good anti-foaming and air release properties

- Highly shear stable

- Good demulsification characteristics

- Excellent anti-wear performance

- High oxidation resistance and thermal stability

- Suitable for all hose materials used with mineral oil based hydraulic oils

PERFORMANCE SPECIFICATIONS

| ORGANISATION | SPECIFICATION |
| --- | --- |
| DIN | 51524 Part 2 |
| ASTM | D6158 |
| Eaton | 35VQ25 |
| Bosch Rexroth | RE90220 |
| Sperry Vickers | I-286-S |
| Cincinnati Milacron | P-68 (ISO 32), P-70 (ISO 46), & P-69 (ISO 68) |
| ISO | 1158 |
| SAE | MS 1004 |
| AFNOR | NFE 48603 (HM) |
| GM | LS-2 (ISO 22-68) |
| Denison | HF-0, HF-1, HF-2 |

TYPICAL PHYSICAL DATA

| HYLOAD ZF ISO VISCOSITY GRADE: | 5 | 10 | 15 | 22 | 32 | 46 | 68 | 100 | 150 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Specific Gravity @ 15.6°C | 0.827 | 0.849 | 0.861 | 0.868 | 0.874 | 0.894 | 0.882 | 0.888 | 0.890 |
| Kinematic Viscosity @ 40°C (cSt) | 5.00 | 10.00 | 15.0 | 22.0 | 32.0 | 46.0 | 68.0 | 100.0 | 150.00 |
| Kinematic Viscosity @ 100°C (cSt) |  |  | 3.40 | 4.30 | 5.40 | 6.78 | 8.82 | 11.35 | 14.80 |
| Viscosity Index |  |  | 96 | 99 | 101 | 101 | 102 | 101 | 99 |
| Flash Point °C | 149 | 165 | 185 | 197 | 214 | 218 | 225 | 231 | 239 |