OIL UK BIO CHAINSAW OIL 68 & 220 HIGH PERFORMANCE BIODEGRADABLE HEAVY CHAINSAW OILS

DESCRIPTION

OIL UK BIO CHAINSAW OILS are highly stable, non-toxic product which have excellent lubricity. They are environmentally friendly and will not harm forests or watercourses. BIO CHAINSAW OILS are excellent heavy duty, non-toxic lubricants which combines biodegradability with outstanding performance. They have outstanding oxidation resistance and non-fling properties. Specialised additives help reduce wear on chainsaw blades and provide excellent oxidation resistance which prevents the build-up of unwanted deposits.

APPLICATION

OIL UK BIO CHAINSAW OILS are suitable for all types of pressure fed chainsaws.

| TYPICAL PHYSICAL DATA |
| --- |
| PROPERTY | UNIT | BIO CHAINSAW OIL 68 | BIO CHAINSAW OIL 220 |
| Appearance |  | Light Amber | Light Amber |
| ISO Grade |  | 68 | 220 |
| Specific Gravity @ 15.6°C | g/ml | 0.880 | 0.917 |
| Kinematic Viscosity @ 100°C | cSt | 14.0 | 48.09 |
| Kinematic Viscosity @ 40°C | cSt | 68.2 | 220.3 |
| Viscosity Index |  | >220 | 276 |
| Flash Point | °C | >200 | >210 |
| Pour Point | °C | -27 | -25 |
| Biodegradability (CEC-L-33-T-82) | % | >90 | >98 |