DESCRIPTION

OIL UK ANGLO-MAX ULTRA RACING 0W-40 is a new generation ultra-high performance, fully synthetic, top tier engine oil designed to meet the most exacting demands of modern engine designs.  Anglo-Max Ultra Racing 0W-40 is an intricate blend of synthetic esters, highly branched isoparaffinic polyalphaolefins, pour point depressant, viscosity modifier and a specialised additive package, designed to give outstanding performance and engine protection. This superb engine oil is designed to maximise performance by providing very high levels of thermal and oxidation stability, engine cleanliness and component wear protection even under the most severe driving and stress conditions.

APPLICATIONS

OIL-UK ANGLO-MAX ULTRA RACING 0W-40 is suitable for high performance vehicles, including those with turbocharged, supercharged and naturally aspirated engines.

Typical oil change intervals (Always adhere to vehicle manufacturer’s recommendation)

| CONDITIONS: | SEVERE | DIFFICULT | MODERATE | GOOD |
| --- | --- | --- | --- | --- |
| KMS: | 10,000 | 20,000 | 30,000 | 40,000 |

FEATURES AND BENEFITS

- Exceptional low temperature properties

- Improved performance

- Fuel economy savings

- Peak performance throughout even the longest service intervals

- Unsurpassed levels of engine protection

PERFORMANCE SPECIFICATIONS

API SN/CF, ACEA A3/B4

VW 502.00/505.00, MB 229.3, 229.5, BMW Longlife-01, Renault RN0700/0710, Porsche A40, Ford WSS-M2C-937-A

| TYPICAL PHYSICAL CHARACTERISTICS |
| --- |
| Appearance | Clear & Bright |
| Specific Gravity @ 15.6˚C 0.848 | 0.841 |
| Kinematic Viscosity @ 100˚C (cSt) | 13.50 |
| Kinematic Viscosity @ 40˚C (cSt) | 76.20 |
| Viscosity Index | 184 |
| Flash Point (°C) | 230 |
| Pour Point (°C) | -45 |
| TBN (mg KOH / g) | 10.20 |