DESCRIPTION

OIL UK ANGLO-MAX SUPER HD MONOGRADES are manufactured from highly refined, high viscosity index base oils and carefully balanced additives producing high quality petrol and diesel engine oils. They offer excellent high temperature stability and stay in grade performance. The latest unique additives used in these grades reduce the unwanted gums and varnishes in cylinders, on pistons and in turbo chargers. They are blended to varying viscosities to suit a wide range of applications.

APPLICATION

OIL UK ANGLO-MAX SUPER HD MONOGRADES may be used in normally aspirated and turbo charged diesel and petrol engines in selected plant equipment, compressors, industrial and hydraulic transmission applications.

Anglo-Max Super HD Monogrades are miscible with all synthetic and mineral based engine oils

Typical oil change intervals (Always adhere to vehicle manufacturer’s recommendation)

| CONDITIONS: | SEVERE | DIFFICULT | MODERATE | GOOD | VERY GOOD |
| --- | --- | --- | --- | --- | --- |
| KMS: | 5,000 | 10,000 | 15,000 | 20,000 | 25,000 |

FEATURES AND BENEFITS

- Good levels of engine protection

- Suitable for a wide range of applications

- Excellent sludge control

PERFORMANCE SPECIFICATIONS

API SG/CF-4/CF

MB 227.0, Caterpillar TO-2, US Military MIL-L-2104E

| TYPICAL PHYSICAL DATA |
| --- |
| PROPERTY | 10W | 20W | 30 | 40 | 50 |
| Specific Gravity @ 15.5°C | 0.880 | 0.885 | 0.889 | 0.891 | 0.894 |
| Kinematic Viscosity @ 100°C (cSt) | 5.29 | 6.42 | 11.14 | 14.55 | 17.61 |
| Kinematic Viscosity @ 40°C (cSt) | 31.31 | 42.00 | 97.14 | 142.02 | 194.02 |
| Viscosity Index | 100 | 101 | 9 | 100 | 108 |
| Flash Point (Open) (°C) | 210 | 215 | 220 | 224 | 230 |
| Total Base Number (mg KOH / g) | 9.07 | 9.09 | 9.01 | 9.08 | 9.05 |