OIL UK GEARLUBE 75W-80 S-ZF HEAVY DUTY FULLY SYNTHETIC COMMERCIAL VEHICLE GEAR OIL

DESCRIPTION

OIL UK GEARLUBE 75W-80 S-ZF is a new fully synthetic gear oil designed for use in a wide variety of commercial vehicle manual transmissions. It provides extended oil drain performance and excellent component protection even under arduous conditions.

APPLICATION

OIL UK GEARLUBE 75W-80 S-ZF is recommended for use in all types of ZF manual and automated manual transmissions fitted to commercial vehicles. This includes AS Tronic, eTronic, Ecosplit, Ecomid and Ecolite units which makes GEARLUBE 75W-80 S-ZF an ideal choice for use in DAF, Iveco, MAN and Renault trucks which employ these systems.

In addition, GEARLUBE 75W-80 S-ZF is recommended for use in commercial vehicle transmissions where any of the following specifications are required. This further broadens its scope of application to many models of Volvo, Mercedes and others.

FEATURES AND BENEFITS

- Very long service life

- Excellent oxidative and thermal stability

- Outstanding low and high temperature performance

- Excellent gear and bearing pitting resistance

- High level of wear protection

- Compatible with a variety of synchroniser materials

- Fuel saving benefits

PERFORMANCE SPECIFICATIONS

ZF:  TE-ML 01L, 02L, 08, 16K TE-ML 02A, 02B, 02D, 02E

MAN 341 Type Z-4, Z-3, Z-2, Z-1 341 Type E-3, E-2, E-1, 341 ML, 341 N

Volvo 97305, 97307, MB 235.4, Eaton Europe 300,000 km or 3 years

API GL-4, US Military MIL-L-2105

OIL UK GEARLUBE 75W-80 S-ZF HEAVY DUTY FULLY SYNTHETIC COMMERCIAL VEHICLE GEAR OIL

| TYPICAL PHYSICAL DATA |
| --- |
| PROPERTY | UNIT | TEST METHOD | TYPICAL DATA |
| Specific Gravity @ 15.5°C | g/ml | ASTM D4052 | 0.859 |
| Kinematic Viscosity @ 100°C | cSt | ASTM D445 | 9.60 |
| Kinematic Viscosity @ 40°C | cSt | ASTM D445 | 56.40 |
| Viscosity Index |  | ASTM D2270 | 155 |
| Flash Point (Open) | °C | ASTM D92 | 215 |
| Pour Point | °C | ASTM D97 | -39 |