PRODUCT DESCRIPTION AND PERFORMANCE SPECIFICATION

OIL UK DOT 5.1 ESP 260/180 DOT 5.1 Brake Fluid is an outstanding product combining two of the highest specifications yet published in one product. This gives it wider applicability than any other brake fluid. It allows Stability Program (ESP) systems to operate effectively over a wide temperature range while maintaining the high temperature performance of a DOT 5.1 fluid. Suitable for all ESP and other conventional brake systems using Glycol Ether based Brake Fluids.

The product shall fully meet the requirements of the latest issue of the US FMVSS 116 DOT 5.1, DOT 4, DOT 3, SAE J 1703, SAE J 1704 and ISO 4925 (Classes 3, 4, 5.1 & 6) Specifications.

| TYPICAL PHYSICAL CHARACTERISTICS |  |
| --- | --- |

| Test Required |  | Typical Results | Specification |
| --- | --- | --- | --- |
| Dry Equilibrium Reflux Boiling Point, °C | 268 | 260 °C. Min. |
| Wet Equilibrium Reflux Boiling Point, °C | 183 | 180 °C. Min. |
| Kinematic Viscosity | @ -40 °C, cSt | 712 | 750 cSt Max. |
|  | @ 100 °C, cSt | 2.04 | 1.5 cSt Min. |
| pH |  | 7.90 | 7 – 11.5 |
| High Temperature Stability, °C | -1 | +/- 3.0 °C. Max |
| Chemical Stability, °C |  | +1 | +/- 3.0 °C. Max |
| Evaporation, %w/w |  | 65 | 80% Max |
| Fluidity & Appearance | @ -40 °C | Pass, 2 seconds | No freezing, Bubble time 10 sec. Max |
|  | @ -50 °C | Pass, 4 seconds | No freezing, Bubble time 35 sec. Max |
| Water Tolerance | @ -40 °C | Clear, 2.5 seconds | 10 seconds Max |
|  | @ +60 °C | Clear, No sediment | Sediment not to exceed 0.05% v/v |
| Compatibility | @ -40 °C | Clear, No stratification | No stratification |
|  | @ +60 °C | Clear, No sediment | Sediment not to exceed 0.05% v/v |
| Colour, visual |  | Pale Straw | Water white to amber |
| Water Content, % |  | < 0.15 | Not required |
| Density @ 20 °C, g/ml |  | 1.067 | Not required |