PRODUCT DESCRIPTION

OIL UK ANGLO-MAX SUPER XHD E7 15W-40 is a superior High Performance engine oil formulated to meet the severe lubrication requirements demanded by heavy, medium and light duty diesel and gasoline engines.

APPLICATIONS

Anglo-Max Super XHD-E7 15W-40 is suitable for normally aspirated and turbocharged diesel and petrol engines. It may be used in heavy duty commercial vehicles such as trucks and buses as well as vans and passenger cars.

Anglo-Max Super XHD-E7 15W-40 is also suitable for off-highway construction plant such as earth moving equipment and tractors, and stationary plant such as heavy duty power generators.

This product is the first choice for a wide variety of major International trucks and buses used for inter-city or long haul applications, where an oil needing to satisfy the requirements of Euro 4 and certain Euro 5 engines is called for. This super high performance product is at the forefront of heavy duty diesel engine oil technology meeting API CI-4/SL and ACEA E7.

Manufacturers include: Cummins, Mercedes Benz, Renault, DAF, Global, Mack, MAN, MTU, Perkins, Scania and Volvo, Caterpillar, and Detroit Diesel.

Typical oil change intervals (Always adhere to vehicle manufacturer’s recommendation)

| CONDITIONS: | SEVERE | DIFFICULT | MODERATE | GOOD | VERY GOOD |
| --- | --- | --- | --- | --- | --- |
| KMS: | 25,000 | 40,000 | 55,000 | 65,000 | 80,000 |

PERFORMANCE LEVEL SPECIFICATIONS

API CI-4/SL, CF

ACEA E7, A3/B3, A3/B4

Mercedes Benz 228.3, 229.1

Cummins CES 20078, CES 20071/72/76/77

MAN M3275

MTU Type 2

Mack EO-N, EO-M Plus

Volvo VDS-3

Renault RVI RLD-2, RLD,

Global DHD-1

ZF TE-ML 04C / 07C

Caterpillar ECF-2, ECF-1-a

Allison C4

Detroit Diesel DDC 93K215

JASO DH-1

Deutz DQC III-10

FEATURES AND BENEFITS

- Outstanding Protection – Anglo-Max Super XHD-E7 15w-40 features an exclusive additive system to ensure maximum soot handling, excellent wear protection and extra-long oil life providing 60,000 km average oil change periods in moderate to good conditions, and up to 80,000kms in very good conditions..

- High Performance – Anglo-Max Super XHD E7 15w-40 adapts and protects under the full range of pressures and temperatures found in modern engines, including those operating constantly in high ambient temperatures.

- Improved Engine Cleanliness – The latest generation additive system in Anglo-Max Super XHD-E7 15w-40 delivers improved engine cleanliness and protection against piston deposits.

- Manufacturers Standards – Anglo-Max Super XHD-E7 15w-40 satisfies and exceeds the most demanding performance standards of major international engine manufacturers and oil and motor vehicle industry specifications.

TYPICAL PHYSICAL DATA

| Test | Units | Test Method | Typical Properties |
| --- | --- | --- | --- |
| Appearance |  | Visual | Clear and Bright |
| Specific Gravity @ 15.5°C |  |  | 0.887 |
| Kinematic Viscosity @ 100°C | cSt | ASTM D445 | 14.6 |
| Kinematic Viscosity @ 40°C | cSt | ASTM D445 | 110.0 |
| Viscosity Index |  | ASTM D2270 | 140 |
| Flash Point (Open) | °C | ASTM D92 | 230 |
| Pour Point | °C | ASTM D97 | -35 |
| Total Base Number | mg KOH/g | ASTM D2986 | 11.2 |