PRODUCT DESCRIPTION AND PERFORMANCE SPECIFICATION

OIL UK DOT 5 260/180 is a high performance Silicone based Hydraulic Brake and Clutch Fluid which fully meets the requirements of the latest issue of the US FMVSS 116 DOT 5 Specification.

| TYPICAL PHYSICAL CHARACTERISTICS |  |
| --- | --- |

| Test Required |  | Typical Results | Specification |
| --- | --- | --- | --- |
| Dry Equilibrium Reflux Boiling Point, °C | >300 | 260 °C. Min. |
| Wet Equilibrium Reflux Boiling Point, °C | >220 | 180 °C. Min. |
| Kinematic Viscosity | @ -40 °C, cSt | 150 | 900 cSt Max. |
|  | @ 100 °C, cSt | 13.9 | 1.5 cSt Min. |
| High Temperature Stability, °C | Nil | +/- 3.0 °C. Max |  |
| Fluidity & Appearance | @ -40 °C | Pass, 1 second | o freezing, Bubble time 10 sec. Max |
|  | @ -50 °C | Pass, 1 second | No freezing, Bubble time 35 sec. Max |
| Water Tolerance | @ -40 °C | Clear, 2 seconds | 10 seconds Max |
|  | @ +60 °C | Clear, No sediment | Sediment not to exceed 0.05% v/v |
| Compatibility | @ -40 °C | Clear, No stratification | No stratification |
|  | @ +60 °C | Clear, No sediment | Sediment not to exceed 0.05% v/v |
| Colour, visual |  | Purple | Purple |