PRODUCT DESCRIPTION AND PERFORMANCE SPECIFICATION

Oil UK DOT 3 260/140 is a high quality Hydraulic Brake and Clutch Fluid which fully meets the requirements of the latest issue of the US FMVSS 116 DOT 3, SAE J 1703 and ISO 4925 (Class 3) Specifications.

| TYPICAL PHYSICAL CHARACTERISTICS |  |
| --- | --- |

| Test Required |  | Typical Results | Specification |
| --- | --- | --- | --- |
| Dry Equilibrium Reflux Boiling Point, °C | 269 | 260 °C. Min. |
| Wet Equilibrium Reflux Boiling Point, °C | 151 | 140 °C. Min. |
| Kinematic Viscosity | @ -40 °C, cSt | 1261 | 1500 cSt Max. |
|  | @ 100 °C, cSt | 2.19 | 1.5 cSt Min. |
| pH |  | 8.90 | 7 – 11.5 |
| High Temperature Stability, °C | Nil | +/- 3.0 °C. Max |
| Chemical Stability, °C |  | +0.5 | +/- 3.0 °C. Max |
| Evaporation, %w/w |  | 61 | 80% Max |
| Fluidity & Appearance | @ -40 °C | Pass, 3 seconds | No freezing, Bubble time 10 sec. Max |
|  | @ -50 °C | Pass, 6 seconds | No freezing, Bubble time 35 sec. Max |
| Water Tolerance | @ -40 °C | Clear, 3 seconds | 10 seconds Max |
|  | @ +60 °C | Clear, No sediment | Sediment not to exceed 0.05% v/v |
| Compatibility | @ -40 °C | Clear, No stratification | No stratification |
|  | @ +60 °C | Clear, No sediment | Sediment not to exceed 0.05% v/v |
| Colour, visual |  | Pale Amber | Water white to amber |
| Water Content, % |  | < 0.20 | Not required |
| Density @ 20 °C, g/ml |  | 1.032 | Not required |