High quality water soluble rust preventative concentrate

PRODUCT DESCRIPTION

OIL UK NO RUST S is an ethanolamine, secondary amine free and boron free synthetic corrosion inhibitor. This product provides excellent ferrous & multi-metal corrosion protection. Additionally, the No Rust S provides tremendous environmental friendly attributes since it is readily biodegradable.

### OIL UK NO RUST S forms an excellent long life clear emulsion when mixed with water, and contains special vapour phase inhibitors to assist corrosion protection to protect sealed systems. This product should be used at dilutions of between 3% and 5%.

FEATURES AND BENEFITS

- Fully synthetic and free from mineral oil

- Readily biodegradable

- Renewable raw material base

- Easy to maintain

- Excellent ferrous corrosion protection

- Excellent multi-metal corrosion protection

- Low fluid residue formation

- Low Foaming Characteristics

- Excellent anti-corrosion properties

- Operator Acceptability

TYPICAL PHYSICAL DATA

| Appearance | Yellow amber liquid |
| --- | --- |
| Specific Gravity @ 20°C | 1.17 |
| Boron Content (%wt) | Nil |
| Product Stability (0/50ºC) | Stable |
| pH @ 5% dilution in deionised water | 8.2 |
| IP 287 Corrosion break point (% volume) | 1.0 |
| IP 125 Corrosion break point (% volume) | 1.0 |
| Aluminum Stain Test | No Stain |
| Copper Stain Test | No Stain |
| Refractive Index | 1.2 |