DESCRIPTION

OIL UK SOLCUT 200 XF is a high performance Semi Synthetic, formaldehyde release biocide free, watermix fluid designed for multi-purpose machining operations. OIL UK SOLCUT 200 XF is a medium oil content product containing selected lubricity additives which give excellent cutting performance and surface finish.

SOLCUT 200 XF is extremely low foaming and works well in soft and hard water areas. It is well suited for use on a variety of steel alloys and can be used for the machining of non-ferrous alloys.

SOLCUT 200 XF is a robust coolant and gives extended service life in the most difficult conditions.

FEATURES AND BENEFITS

- Enhanced Health and Safety - Formaldehyde free

- Enhanced tool life and excellent surface finish

- Suitable for both multiple moderate applications

- Low foaming tendency in high pressure systems and suitable for both hard and soft water qualities

- Multi-metal compatible. Suitable for both ferrous and non-ferrous materials

- Provides long, low odour coolant life and excellent machine tool cleanliness

- Excellent cost saving potential through enhanced tool life

- Extra high levels of corrosion protection

MATERIAL SUITABILITY AND RECOMMENDED CONCENTRATIONS

| Material Type | Performance Rating | Recommended Concentration General Purpose | Recommended Concentration Heavy Duty |
| --- | --- | --- | --- |
| Aluminium Alloys | XXXX | 5-7% | 8-10% |
| High Alloy/Stainless Steels | XXX | 5-7% | 8-10% |
| Low to medium tensile steels | XXXXX | 5-7% | 8-10% |
| Copper/Brass | XXXX | 5-7% | 8-10% |
| Cast Iron | XXX | 4-6% | 5-8% |
| Machining Operations |  |  |
| Turning, Milling Drilling | 4-6% | 7-8% |
| Surface & cylindrical grinding operations | 3-5% |

TYPICAL PHYSICAL PROPERTIES

| Appearance - Emulsion | Semi Translucent |
| --- | --- |
| pH at 5% in distilled water | 9.3 |
| IP 287 Corrosion break point | 2.5 |
| Refractometer correction factor | 1.4 |