DESCRIPTION

OIL UK SOLCUT 100 XF is a Semi Synthetic, formaldehyde release biocide free, watermix fluid designed to perform in general purpose applications with a wide range of material suitability. The low oil content of this product makes it well suited to the machining of cast iron.

OIL UK SOLCUT 100 XF is an extremely low foaming product and works equally well in both hard and soft waters. It is also an extremely robust coolant and gives extended service life in the most difficult conditions.

FEATURES AND BENEFITS

- Enhanced Health and Safety - Formaldehyde free

- Loaded with lubricity components for enhanced tool life and excellent surface finish

- Low foaming tendency in high pressure systems and suitable for both hard and soft water qualities

- Particularly Suitable for both ferrous metals and cast iron

- Provides long, low odour coolant life and excellent machine tool cleanliness

- Excellent cost saving potential through enhanced tool life

- Extra high levels of corrosion protection

MATERIAL SUITABILITY AND RECOMMENDED CONCENTRATIONS

| Material Type | Performance Rating | Recommended Concentration General Purpose | Recommended Concentration Heavy Duty |
| --- | --- | --- | --- |
| Aluminium & Titanium Alloys | XXX | 5-7% | 8-10% |
| High Alloy/Stainless Steels | XXXX | 5-7% | 8-10% |
| Low to medium tensile steels | XXXX | 5-7% |  |
| Copper/Brass | XX | 5-7% | 8-10% |
| Cast Iron | XXXXX | 4-6% | 5-8% |
| Machining Operations |  |  |
| Turning, Milling Drilling | 4-6% | 7-8% |
| Tapping & Threading | 5-8% | 9-12% |
| Surface, cylindrical & centreless grinding operations | 3-4% |

TYPICAL PHYSICAL PROPERTIES

| Appearance - Emulsion | Translucent |
| --- | --- |
| pH at 5% in distilled water | 9.4 |
| IP 287 Corrosion break point | 2.5 |
| Refractometer correction factor | 2.0 |