PRODUCT DESCRIPTION

OIL UK SUPER UNIVERSAL TRACTOR OIL 15W-30 is suitable for engines, transmissions, hydraulics and final drives.
The latest agricultural machinery in the modern intensive farming environment needs the protection of a high quality lubricant. Oil UK Super Universal Tractor Oil 15w-30 is blended from carefully selected base oils and the latest in additive technology to produce a lubricant for the demands of most farm equipment. The latest additives used help reduce wet brake noise. The carefully selected base oils ensure protection even under the most arduous of conditions.

APPLICATIONS

OIL UK SUPER UNIVERSAL TRACTOR OIL 15W-30 is suitable for use in both normally aspirated and turbocharged diesel and petrol engines, transmission systems including those fitted with wet brakes, hydraulic systems, oil immersed clutches, gearboxes and final drives. It is suitable for agricultural, plant and off road machinery.
PERFORMANCE LEVEL SPECIFICATIONS

API CE/SF (Engine), GL-4 (Gears),
CCMC D4/G2, MB 227.1,
Massey Fergusson 1135, 1127, 1139
Ford M2C 86A, 134B/C, 159B Allison C4,
John Deere J20A, ZF TE ML 06B, 06L, 07B, 07D, Caterpillar TO-2

TYPICAL PHYSICAL DATA

Test	Units	Test Method	Typical Properties
Specific Gravity @ 15.5°C	g/ml	ASTM D4052	0.883
Kinematic Viscosity @ 100°C	cSt	ASTM D445	11.49
Kinematic Viscosity @ 40°C	cSt	ASTM D445	85.04
Viscosity Index		ASTM D2270	125
Flash Point (COC)	°C	ASTM D92	218
Pour Point	°C	ASTM D97	-31
Total Base Number	mg KOH/g	ASTM D2986	10.38